# X-ray diffraction investigation of structure of gold nanorods and metal oxide nanoparticles for theranostic applications

## G. Opiła1, M. Kasprzyk2, A. Pietrzyk2, Janusz Przewoźnik1, E. Gumieniczek-Chłopek3, A. Karewicz2, J. Dulińska-Litewka4, Stanisław Rumian5, 6, 7, Szczepan Zapotoczny2, Cz. Kapusta1

## *1AGH University of Krakow, Faculty of Physics and Applied Computer Science, al. A. Mickiewicza 30, 30-059 Krakow, Poland, 2Jagiellonian University, Faculty of Chemistry, ul. Gronostajowa 2, 30-387 Krakow, Poland 3Jerzy Haber Institute of Catalysis and Surface Chemistry, Polish Academy of Sciences, Niezapominajek 8, 30-239, Krakow, Poland, 4Chair of Medical Biochemistry, Jagiellonian University Medical College, Św. Anny 12, 31-008, Krakow, Poland, 5Interuniversity Center for New Techniques and Medical Technologies, Cracow University of Technology, Warszawska 24, 31-155 Kraków, Poland, 6St. John Paul II Cracow Specialist Hospital, ul. Prądnicka 80, 31- 202 Kraków, 7Academy of Applied Sciences in Nowy Sącz, ul. Staszica 1, 33–300 Nowy Sącz.*

### gopila@agh.edu.pl

Magnetic and plasmonic nanoparticles can be used in medicine, for example as theranostic agents, combining diagnostic and therapeutic processes. Plasmonic nanoparticles exhibit qualities that make them perfectly suited for sensing, including biosensing. For determination of their properties, it is important to know their composition and structure, as it can affect their efficiency in their respective tasks. X-ray diffraction (XRD) can help to determine the crystallographic structures and phase content of the nanoparticles as well as to estimate the size of the nanocrystallites.

We have obtained diffractograms for iron oxide nanoparticles synthesized by coprecipitation of iron (II) and iron (III) chlorides in the presence of hyaluronic acid sodium salt (Na-HA), as described by Kasprzyk et al. 2025 [1] and for gold nanorods with plasmonic properties, synthesized using a modified seedless growth technique described by Ali et al. 2012 [2]. Then, we have determined mean diameter of the nanoparticles using the Williamson-Hall method and imaged the nanoparticles using Scanning Transmission Electron Microscopy (STEM), which allowed for a comparison between a direct and indirect size estimation. For the gold nanorods a conclusion on the anisotropic growth was drawn.

For plasmonic nanoparticles, their dimensions and material influence their absorption spectra, and, consequently the efficiency of photothermal conversion caused by localised surface plasmon resonance (LSPR). Size and composition are also crucial for superparamagnetic iron oxide nanoparticles (SPIONs), as they decide on their superparamagnetic properties. Thermographic measurements of a suspension of gold nanorods illuminated with 450 mW, 808 nm laser light will be demonstrated and compared to analogous measurements of a suspension of spherical gold nanoparticles. For SPIONs, magnetic measurements such as Vibrating Sample Magnetometry (VSM) results will be shown. The relationship between properties that can be derived from diffractogram analysis and their consequences for application purposes will be discussed.

[1] Kasprzyk, M., Opiła, G., Hinz, A., Stankiewicz, S., Bzowska, M., Wolski, K., Dulińska-Litewka, J., Przewoźnik, J. Kapusta, Cz., Karewicz, A. (2025). ACS Appl. **17**, 9059-9073.

#### [2] Ali, M. R. K., Snyder, B., El-Sayed, M. A. (2012). Langmuir 28, 9807-9815.

The research has been supported by a grant (WSPR.WCh.1.10.2022.6(1)) from the Priority Research Area (Sci-Mat) under the Strategic Programme Excellence Initiative at Jagiellonian University and Narodowe Centrum Nauki (NCN) OPUS grant no. 2020/39/B/NZ5/03142. Gabriela Opiła, Janusz Przewoźnik and Czesław Kapusta acknowledge support by the program “Excellence initiative−research university” for the AGH University of Krakow.